Deeper Insights
Unveiling Dopant Profiles with GIXRD

---
Definitions
- Dopant
- Doped
- XRD
- GIXRD
- Amorphous
- Crystalline
- Amorphous hump

---
Background (Solids)
Two types of generalized solids
Amorphous (left)
Crystalline (right)

---
Background (Doping)

---
Background (Atomic Planes)

---
Background (Samples)
Two types of generalized solids
Amorphous (left)
Crystalline (right)

---
Background (XRD/GIXRD)
X-Ray Diffraction utilizes x-rays of Cu Kα wavelength (1.54Å)
Uses Bragg’s law:
2dsinθ=nλ
Diminishes according to:
I(y)=I0e−α y

---
Background (Single Crystal XRD)

---
Methods (Method 1)
Takes the highest value from the amorphous hump, and the highest value from the crystalline peak to find the ratio
Omega	Amorphous Range	Crystalline Range
6	13-33	60-63
5	12-31	59-61
3	14-35	36-38
m=\frac{I_a}{I_a+I_c}

---
Methods (Methods 2&3)
Curve Fit
Fits standard Gaussian function
Amorphous is yellow
Crystalline is green
Summation
Numerical integration on the regions

---
Analysis

---
Analysis

---
Conclusion
- Samples of dopant silicon with phosphorous were analyzed
- GIXRD was used to probe doped samples with x-rays to provide a diffractogram
- Three methods were used to analyze composition of doped samples using intensity, curve fitting, and summation
- The methods come close in their agreement for depth of how far the dopant penetrated into the sample

---
Future Work

---
References