Deeper Insights
Unveiling Dopant Profiles with GIXRD
Mark Smith
Advisor: Brother Oliphant
Brigham Young University-Idaho

---
Background (Definitions)
- Dope
  - Adding a substance to a material to change certain characteristics about that material
- Dopant
  - Substance doing the doping

---
Background (Definitions)
- X-Ray Diffraction (XRD)
  - Broad category of techniques that shine x-rays at a sample to determine a variety of characteristics such as composition
  - There are powder and single crystal diffraction methods
- Grazing Incidence X-Ray Diffraction (GIXRD)
  - Specific type of XRD technique that uses single crystal XRD in order to have the x-rays only probe near the surface of the sample
  - This leaves the sample intact, preserving the layers

---
Background (XRD/GIXRD)
X-Ray Diffraction utilizes x-rays of Cu Kα wavelength (1.54Å)
Uses Bragg’s law:
2dsinθ=nλ
Diminishes according to:
I(y)=I0e−α y

---
Background (Atomic Planes)
When x-rays interact with bulk samples, all atomic planes participate in the resulting diffraction.

---
Background (Solids)
Two types of generalized solids
Amorphous (left)
Crystalline (right)

---
Background (Solids; Crystalline)
Crystalline
  Type of material structure in which the atoms arrange themselves in a regular infinity repeatable pattern

---
Background (Solids; Crystalline)
Crystalline Peak
  Pattern Produced by crystalline parts of a material under XRD

---
Background (Solids; Amorphous)
Amorphous
  Type of material structure in which the atoms do not form an infinite repeatable pattern

---
Background (Solids; Amorphous)
Amorphous Hump
  Pattern produced by amorphous parts of a material under XRD

---
Background (Sample)
In this work samples of silicon that were doped with phosphorous were used. These were provided by the semiconductor team from their earlier doping trials.

---
Background (Samples)
The doped samples have an atomic similar to what is shown here.
This leads to a superposition-like diffractogram

---
Background (Single Crystal XRD)
- Single crystal XRD leaves the sample intact, with the plane of atoms aligned in their preferred orientation
- This means alignment is everything

---
Methods (Method 1)
Takes the highest value from the amorphous hump, and the highest value from the crystalline peak to find the ratio
Omega	Amorphous Range	Crystalline Range
6	13-33	60-63
5	12-31	59-61
3	14-35	36-38
m=\frac{I_a}{I_a+I_c}

---
Methods (Methods 2&3)
Curve Fit
Fits standard Gaussian function
Amorphous is yellow
Crystalline is green
Summation
Numerical integration on the regions

---
Analysis

---
Conclusion
- Samples of dopant silicon with phosphorous were analyzed
- GIXRD was used to probe doped samples with x-rays to provide a diffractogram
- Three methods were used to analyze composition of doped samples using intensity, curve fitting, and summation
- The methods come close in their agreement for depth of how far the dopant penetrated into the sample

---
Future Work
- The Surface Physics group is building a deposition machine that will have an oscillator in their to determine layer thickness to compare to
- Nonuniform layers to get individualized layer composition

---
References
- A. Pandey, S. Dalal, S. Dutta, and A. Dixit, “Structural characterization of polycrystalline thin films by X-ray diffraction techniques,” Journal of Materials Science: Materials in Electronics 32, 1341–1368 (2021).
- G. L. Parks, M. L. Pease, A. W. Burns, K. A. Layman, M. E. Bussell, X. Wang, J. Hanson, and J. A. Rodriguez, “Characterization and hydrodesulfurization properties of catalysts derived from amorphous metal-boron materials,” Journal of Catalysis 246, 277–292 (2007).
- P. Colombi, P. Zanola, E. Bontempi, and L. E. Depero, “Modeling of glancing incidence X-ray for depth profiling of thin layers,” Spectrochimica Acta Part B: 14 BIBLIOGRAPHY 15 Atomic Spectroscopy 62, 554–557 (2007), a Collection of Papers Presented at the 18th International Congress on X-Ray Optics and Microanalysis (ICXOM 2005).
- B. L. Henke, E. M. Gullikson, and J. C. Davis, “X-ray interactions: photoabsorption, scattering, transmission, and reflection at E=50-30000 eV, Z=1-92,” Atomic Data and Nuclear Data Tables 54, 181–342 (1993).

---
References
- E. Hecht, Optics, 4th intern ed. (Addison Wesley, 2002).
- C. Achilles et al., “AMORPHOUS PHASE CHARACTERIZATION THROUGH X-RAY DIFFRACTION PROFILE MODELING: IMPLICATIONS FOR AMORPHOUS PHASES IN GALE CRATER ROCKS AND SOILS.,” In 49th Lunar and Planetary Science Conference 2018 (LPI Contrib. No. 2083), 2083 (2018).
- A. van Riessen, E. Jamieson, H. Gildenhuys, R. Skane, and J. Allery, “Using XRD to Assess the Strength of Fly-Ash- and Metakaolin-Based Geopolymers,” Materials 18 (2025).
- J. Liu, R. E. Saw, and Y.-H. Kiang, “Calculation of effective penetration depth in X-ray diffraction for pharmaceutical solids,” Journal of Pharmaceutical Sciences 99, 3807–3814 (2010).